宁波东方永宁化工科技有限公司www.yongningchem.com



Ningbo Dongfang Yongning Chemical Technology Co;Ltd

宁波东方永宁化工科技有限公司

CERTIFICEATE OF ANALYSIS

质量检验报告单

	Commodity


	Polyquaternium-7

	Batch No.


	202201007
	Analysis Date


	Jan.12th, 2022

	Quantity


	3000KG

	The Results : The sample complies with  Specification.

	Items


	Testing method


	Specifications


	[image: image1.png]R



Results



	Appearance


	Visual method


	Colourless to light yellow transparent liquid


	light yellow transparent liquid

 

	solid content（%）


	105±2℃ 3h
	10±1
	10.10

	pH 

（1% aqueous solution） 


	pH （ 1% aqueous solution）
	5.0-7.0
	5.67

	rotation viscosity（cp/25℃)

	
	8000~25000
	14600


Shelflife:1 year
Inspector: 刘翠娟                     Checker: 王路军
