Henan Deyirui New Material Co., LTD

| Items Product Name |  | Chromatic light | Strength (%) | moisture content（%） | pH value | Iron ion content（ppm） | Conductivity （µs/cm） | External standard (%) | DMF insolubles （%） | Ash content（%） | Pressure value (MPa) | Use |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| General products | Iindex | Approximate, micro | ≥460 | ≤0.5 | 5.0-7.0 | ≤10 | ≤50 | ≥99.0 | ≤0.15 | ≤0.2 | Be without | Filter cake, plastic, color masterbatch |
|  | Random measurement | Approximate, micro | 460 | 0.05 | 5.16 | 6.69 | 35.1 | 99.27 | 0.08 | 0.11 |  |  |
| Fine products | Iindex | Approximate, micro | ≥460 | ≤0.5 | 6.0-8.0 | ≤10 | ≤30 | ≥99.5 | ≤0.1 | ≤0.1 | Be without | Ink, inkjet, digital printing, high end color masterbatch (medicine, aviation) |
|  | Random measurement | Approximate, micro | 460 | 0.03 | 6.23 | 5.36 | 25 | 99.59 | 0.02 | 0.02 |  |  |
| Excellent products | Iindex | Approximate, micro | ≥460 | ≤0.5 | 6.0-8.0 | ≤10 | ≤20 | ≥99.5 | ≤0.1 | ≤0.1 | 0.2 | wire drawing |
|  | Random measurement | Approximate, micro | 460 | 0.01 | 6.21 | 3.28 | 18 | 99.65 | 0.01 | 0.02 | 0.04 |  |

Specific Product Description (Solvent Yellow 114)

产品描述（溶剂黄114）Product Description (Solvent Yellow 114)

溶剂黄114 (Solvent Yellow 114)

分子式 (Molecular Formula): C18H11NO3    分子量 (Molecular Weight): 289.289

CAS NO: 75216-45-4        EINECS NO: 231-474-9

| 检测项目 Items 产品名称 Product Name |  | 色光 Chromatic light | 强度 Strength (%) | 水分 moisture content（%） | PH值 pH value | 铁离子 Iron ion content（ppm） | 电导率 Conductivity （µs/cm） | 外标 External standard (%) | DMF不溶物 DMF insolubles （%） | 灰分 Ash content（%） | 压力值 Pressure value (MPa) | 用 途 Use |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 普品 General products | 指标 Iindex | 近似、微 Approximate, micro | ≥460 | ≤0.5 | 5.0-7.0 | ≤10 | ≤50 | ≥99.0 | ≤0.15 | ≤0.2 | 无 Be without | 滤饼、塑料塑胶、 色母料 Filter cake, plastic, color masterbatch |
|  | 随机实测Random measurement | 近似、微 Approximate, micro | 460 | 0.05 | 5.16 | 6.69 | 35.1 | 99.27 | 0.08 | 0.11 |  |  |
| 精品 Fine products | 指标 Iindex | 近似、微 Approximate, micro | ≥460 | ≤0.5 | 6.0-8.0 | ≤10 | ≤30 | ≥99.5 | ≤0.1 | ≤0.1 | 无 Be without | 墨水、喷墨、数码印花、高端色母（医用、航空）Ink, inkjet, digital printing, high end color masterbatch (medicine, aviation) |
|  | 随机实测Random measurement | 近似、微 Approximate, micro | 460 | 0.03 | 6.23 | 5.36 | 25 | 99.59 | 0.02 | 0.02 |  |  |
| 优品Excellent products | 指标 Iindex | 近似、微 Approximate, micro | ≥460 | ≤0.5 | 6.0-8.0 | ≤10 | ≤20 | ≥99.5 | ≤0.1 | ≤0.1 | 0.2 | 拉丝 wire drawing |
|  | 随机实测Random measurement | 近似、微 Approximate, micro | 460 | 0.01 | 6.21 | 3.28 | 18 | 99.65 | 0.01 | 0.02 | 0.04 |  |