Dongying Haohui Chemical Co., Ltd

4,4'-Oxydianiline

Quality Inspection Report

Batch No.: 220708                             Test date: 2022-07-25

| Inspection items | Product standard | Inspection results |
| --- | --- | --- |
| Appearance | White or yellowish block Crystalline, powder | White block crystal |
| Play a part | ≤0.2% | 0.18% |
| Initial melting point | ≥188.0℃ | 189.0℃ |
| Final melting point | ≥189.8℃ | 191.0℃ |
| Purity | ≥99.5% | 99.80% |
| Conclusion: | Qualified |  |