赵县宏远化工有限公司

Zhaoxian County Hongyuan Chemical Co.,Ltd.

检 验 报 告

ANALYTICAL   REPORT

| 产品名称 Product Name | 氧化铁红 Iron Oxide Red |  |
| --- | --- | --- |
| 型号 Model | Y101 |  |
| 化学名称 Chemical name | 三氧化二铁(Fe2O3·αH20) Ferric Oxide (Fe2O3·αH20) |  |
| 产品形态 Product form | 粉末 Powder |  |
| 颜料索引号 Pigment index number | 颜料红101 (77491) Pigment red 101 (77491) |  |
| CAS NO. / EC NO. | 1309-37-1/215-168-2 |  |
| Specification 规格 | 含量(Fe2O3·αH20) % Content % | ≥96 |
|  | 吸油量 ml/100g Oil absorption ml/100g | 15~25 |
|  | 筛余物325目 % Sieve residue 325 mesh % | ≤0.3 |
|  | 水溶物 % Water soluble matter % | ≤0.3 |
|  | 水份 % Moisture % | ≤1.0 |
|  | PH值 PH value | 3.5~7 |
|  | 挥发物105℃ % Volatile matter 105 ℃ % | ≤1.0 |
|  | 密度 g/cm3 Density g/cm3 | 0.7~1.1 |
|  | 震实密度 g/cm3 Compaction density g/cm3 | 0.5 |
|  | 主要粒子尺寸 μm Main particle size μm | 0.1~0.3 |
|  | 着色力（与标样相比） % Colouring force (compared with standard sample) % | 95~105 |
|  | 色差△E（与标样相比) Color difference △E (compared with standard sample) | ≤1.0 |
| 包装 Packing | 25kg纸袋或编织袋/1000kg吨袋或散装托盘 25kg paper bag or woven bag /1000kg ton bag or bulk tray |  |
| 运输和贮存 Transportation and storage | 为防止风化应贮存在干燥的地方 Store in a dry place to prevent weathering |  |
| 安全 Security | 在欧共体EC1907/2006&EC1272/2008中，此产品没有被归类到危险化学 品中，在运输条例中也不具有危险性。 In EC 1907/2006& EC 1272/2008, this product is not classified as a hazardous chemical, nor is it dangerous in the transport regulations. |  |