Liaoning Flutuo New Energy Materials Co., LTD

Quality inspection report form

| product name | Trifluorocarcinomas |  | source |  |  | storehouse |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| production unit | Liaoning Flutuo New Energy Materials Co., LTD |  | report date |  |  | 2022/07/13 |  |
| sampling time | 202207/13 |  | packing specifications |  |  | 25kg / bag |  |
| examination date | 2022/07/13 |  | quantity |  |  | 16000kg |  |
| result |  |  |  |  |  |  |  |
| lot number |  | surface |  | content 99.0%min | Shuifen 1.0%max |  | Quantity / bag |
| 2022052613 |  | Class white crystal |  | 99.22 | 0.22% |  | 40 |
| 2022052614 |  | Class white crystal |  | 99.23 | 0.03% |  | 40 |
| 2022070902 |  | Class white crystal |  | 99.27 | 0.08% |  | 40 |
| 2022070903 |  | Class white crystal |  | 99.68 | 0.13% |  | 40 |
| 2022071001 |  | Class white crystal |  | 99.22 | 0.22% |  | 40 |
| 2022071002 |  | Class white crystal |  | 99.47 | 0.08% |  | 40 |
| 2022071003 |  | Class white crystal |  | 99.71 | 0.05% |  | 40 |
| 2022071101 |  | Class white crystal |  | 99.64 | 0.07% |  | 40 |
| 2022071102 |  | Class white crystal |  | 99.22 | 0.13% |  | 40 |
| 2022071103 |  | Class white crystal |  | 99.67 | 0.12% |  | 40 |
| 2022071201 |  | Class white crystal |  | 99.22 | 0.05% |  | 40 |
| 2022071202 |  | Class white crystal |  | 99.67 | 0.04% |  | 40 |
| 2022071203 |  | Class white crystal |  | 99.45 | 0.03% |  | 40 |
| 2022071303 |  | Class white crystal |  | 99.23 | 0.05% |  | 40 |
| 2022071302 |  | Class white crystal |  | 99.41 | 0.13% |  | 40 |
| 2022071303 |  | Class white crystal |  | 99.50 | 0.22% |  | 40 |
| Inspection conclusion: this batch of products are qualified. unit stamp |  |  |  |  |  |  |  |
| remarks: |  |  |  |  |  |  |  |

Inspection:, Xie Caihua         Review: Wang Feng         Audit: Liu Yiting

Date of issuance: July 13,2022