Calcium Phosphate hydroxide
Product Name:       Calcium Phosphate hydroxide (TCP)
Other Name:      Hydroxylapatite  (HAP)
Grade:     Tech grade 
Formula:           Ca5(PO4)3OH  
Molecular Weight:      1004
CAS No.: 1306-06-5
Properties.:  Fine white powder, Relative density is 3.18, melting point is 1670 centigrade. Easily soluble in dilute hydrochloric acid and nitric acid. Very slightly dissolved in water and ethyl alcohol.
Application:     Hydroxyapatite, also called hydroxylapatite, alkali type calcium phosphate, calcium is apatite (Ca5 (PO4) (OH) 3) natural mineralized. OH- base can be fluoride, chloride and carbonate ions, generate fluorine apatite or chloride matrix apatite, the calcium ions can be a variety of metal ions by ion exchange reaction, form the corresponding metal ions M apatite (M on behalf of replacing calcium metalions)
Storage conditions:  Store in cool & dry place, Keep away from strong light and heat.

 

	Items 
	Spec

	P2O5,%
	38.5-41.0

	CaO, %
	51.0-55.0

	Moisture, %
	2.5 Max

	PH Value(10g/L) 
	6.0-8.0

	Insoluble in  hydrochloric acid, %
	0.2Max

	Particle Size  
	99.0%Min <38um

	Arsenic ( As2O3),mg/kg
	3.0Max

	Lead ( Pb ),mg/kg
	20.0Max

	Fluoride ( F ),mg/kg
	50.0Max

	Loss on drying(at 105°C), %
	4.5Max

	Loss on Ignition (at 850°C),%
	2.0Max


