SHANDONG WUYANG CHEMICAL CO., LTD

        BeiChen Road , Economic Development Zone, Ling County, Shandong ,China 

               Certificate   Of   Analysis

Product Item: Direct Red 23

Batch Number:               
	 ITEM
	 QUALITY SPECIFICATION
	  RESULT

	APPEARANCE
	PURPLE-RED POWDER
	 PURPLE-RED POWDER

	STRENGTH
	STANDARD 100%
	  100%

	COLORED LIGHT
	SIMILAR AS STANDARD
	SIMILAR AS STANDARD

	WATER INSOLUABILITY
	MAX.1.0%
	   0.55%

	WATER CONTENT
	MAX.7.0%
	  2.00%

	DEGREE OF FINENESS
	MAX.5.0%
	  2.50%


 Date: JAN.9,2022
