| Product Name: 4,4'- diaminodiphenyl ether |  |  |
| --- | --- | --- |
| Production batch No.: 420220619000 | Analysis date: June 19, 2022 |  |
| Test items | Standard requirements | Inspection results |
| appearance | White crystal | White crystal |
| Content% | ≥99.5 | 99.89 |
| Initial melting point | ≥186 | 192.2 |