YIDU JOVIAN INDUSTRY CO., LTD

Inspection Report

Product Name: Benzophenone                              Report date: 2022.07.20

| Inspection Items | Quality Requirement | Detection Result |
| --- | --- | --- |
| Appearance | White flake | Qualified |
| Benzophenone GC content (%) | ≥99.70 | 99.81 |
| Chroma(Platinum cobalt) | ≤70 | 50 |
| Melting range (℃) | 47-49 | 47.9-48.1 |
| Inspection quantity | ton | 0.2 |
| Shipment quantity | ton | 0.2 |