Guangxi Fengshan County Chemical Co., Ltd. Inspection Report

| Product Name: | Food Grade Calcium Carbonate |
| --- | --- |
| Specification: | 400 Mesh |
| Production Date: | June 19, 2024 |
| Batch Number: | 240619 |
| Packaging: | Jumbo Bag (750KG) |
| Quantity: | 120 Bags |
| Inspection Date: | June 19, 2024 |
| Expiration Date: | June 18, 2026 |
| Inspection Standard: | GB18986. 214-2016 |

| Inspection Items | Quality Index (%) | Results (%) | Conclusion |
| --- | --- | --- | --- |
| 1. Appearance and Identification | White Powder | White Powder | Pass |
| 2. Calcium Carbonate Content (Dry Basis) | 98.0-100.50 | 99.12 | Pass |
| 3. Insoluble Acid Content | ≤0.20 | 0.04 | Pass |
| 4. Magnesium and Alkali Metals | Pass | Pass | Pass |
| 5. Heavy Metals (Pb) | ≤1.0 | 0.84 | Pass |
| 6. Lead Content | ≤0.030 | <0.030 | Pass |
| 7. Arsenic Content | ≤0.0003 | 0.000021 | Pass |
| 8. Loss on Drying | ≤2.0 | 0.13 | Pass |
| 9. Fluorine Content | ≤0.005 | 0.00048 | Pass |
| 10. Mercury Content | ≤0.0003 | <0.0003 | Pass |
| 11. Cadmium Content | ≤0.0001 | 0.000021 | Pass |
| 12. Chromium Content | ≤0.0002 | 0.000025 | Pass |
| 13. Iron Content | / | 0.0043 | / |
| 14. Manganese Content | / | 0.0056 | / |
| 15. Whiteness (Reflectance) | ≥94.0 | 96.2 | Pass |
| 16. Fineness | ≥99.0 | 99.8 | Pass |

| Conclusion: The above inspection items comply with GB1886. 214-2016 standards. | Judgment: Pass |
| --- | --- |

| Approved by: |  |
| --- | --- |
| Reviewed by: |  |
| ------------------ | --- |
| Inspected by: |  |