Weifang Zhongqing Fine Chemical Co., Ltd.
Certificate   Of   Analysis
Product Item: Polyaluminium Chloride

	ITEM
	QUALITY SPECIFICATION
	RESULT

	APPEARANCE
	YELLOWWISH BROWN RESINOUS SOLID 
	YELLOWWISH BROWN RESINOUS SOLID

	MASS FRACTION OF ALUMINA  (Al2O3) /% ≥
	29.0
	QUALIFIED

	COLORED LIGHT
	SIMILAR AS STANDARD
	SIMILAR AS STANDARD

	WATER INSOLUABILITY
	MAX.0.6%
	0.55%

	PH (1% AQUEOUS SOLUTION)
	3.5-5.0
	4.3

	MASS FRACTION OF As /% ≤
	0.0006
	--

	MASS FRACTION OF Pb /% ≤
	0.003
	--

	MASS FRACTION OF Cd /% ≤
	0.0006
	--

	MASS FRACTION OF Hg /% ≤
	0.00003
	--

	MASS FRACTION OF (Cr+6) /% ≤
	0.0015
	--


 Date: JAN.20,2022

