Standard: GB/T17529,1-2008

| Item | Grade | Test Result | Stander |
| --- | --- | --- | --- |
| Purity,％ ≥ | 99.5 | 99.80 | GB/T17529. 1-2008 |
| Colour, Hazen≤ | 20 | 10 | GB/T17530. 3-1998 |
| Water Content％ ≤ | 0.20 | 0.09 | GB/T6283-1986 |
| Inhibitor Content(MEHQ) (m/m),10-6 | 200±20 | 190 | GB/T17530.5-1998 |
| Appearance: | Clear Colourless liquid, Odour Pungent smell |  |  |
| Final Result: High-class | Laboratory Technician |  |  |
|  | Checker: |  |  |
| Remark: |  |  |  |