CERTIFICATE OF ANALYSIS

| Items | Standard（Unit） | Test Result（Unit） | Conclusion |
| --- | --- | --- | --- |
| Appearance | White Or Light white grain | White Grain | Qualified |
| Content % | ≥99.5 | 99.6 | Qualified |
| Free Water % | ≤1.2 | 1.1 | Qualified |
| PH（10% Aqueous Solution）% | ≥4.0 | 5.5 | Qualified |
| Insoluble Matter（10% Nitric Acid Solution）% | ≤0.2 | 0.0 | Qualified |
| Average Crushing Force Of Particles | ≥5N/Grain | 7N/Grain | Qualified |
| Granularity % （1.00mm-2.80mm） | ≥85 | 95 | Qualified |