Concrete Admixture – Alkali-Free Accelerator for Shotcrete (GQ-SN03)

Product Name: Alkali-Free Accelerator for Shotcrete (GQ-SN03)
Type: GQ-SN03
Package: 250kg/drum, 1000kg/IBC Tank

Alkali-Free Accelerator for Shotcrete

(GQ-SN03)

Description:

GQ-SN03 is a high-performance alkali-free concrete accelerator for sprayed concrete. It is a liquid form which dosage can be varied as according to the designed setting and hardening times.

Application:

GQ-SN03  is suitable for all applications, where high and early strength, good final strength and extremely thick layers are required.

- Temporary and permanent rock support in tunnels.

- Rock support in mining.

- Poor ground conditions.

- Tunnel linings, cement ground injection and foam concrete which need acceleration of cementitious grouts.

Features:

- Quick setting property allowed with rapid work progress and construct thick sprayed concrete linings via layered application during one construction sequence. Initial setting time is 2 min to 5 min, final setting time is 3min to 10min.

- Good adhesiveness, one spray layer can be 8 mm to 150mm.

- High strength and concrete performance durability.

- Easy handling as well as facilitating accurate addition to concrete.

| Items | Specification |
| --- | --- |
| Form | Liquid |
| Visual Appearance | Beige |
| Density (+20℃) | 1.43 ±0.03g/ml |
| pH value (1:1 water solution) | 2.6±0.5 |
| Viscosity | ＞400mPa.s |
| Thermal stability | +5℃ to +35℃ |
| Chloride | Free |
| Recommended addition rate: 3% to 8%.of cement quantity |  |

- Very low dust production with good working environment.

- Lower handling cost.

Technical Data Sheet

Storage

GQ-SN03 kept in closed containers which made of plastic, glass fiber or stainless steel. The container is 250kg per drum. 1000kg per IBC tank.    The shelf life is 8 months.